[image: image1.jpg]l‘l" KRR R

WINSOME PAINTS CO., LTD.

ERNATBREAGIETBAI P 012042
Room 1204, Yuen Long Trading Centre, 33 Wang Yip Street West, Yuen Long, N.T. Hong Kong.
TEL: 24766844 FAX: 24730017





PRODUCT INFORMATION
PRODUCT CODE
: 
E138
PRODUCT NAME
:
PANDA BRAND ECO CLEAR LACQUER

DESCRIPTION
:
IT IS ONE OF THE TRADITIONAL PRODUCTS WHICH ENJOYS REPUTAION FOR ITS EASY APPLICATION, GLOSSY FILM, QUICK DRYING AND WATER RESISTANCE. IT IS SUITABLE FOR WOOD PRODUCTS, BAMBOO FURNITURE AND YACHT.
VEHICLE
:
SYNTHETIC RESINS
COLOUR 
:
CLEAR LIGHT AMBER

GLOSS
:
FULL GLOSS

DRYING TIME
:
TOUCH DRY           3  HOURS


RECOATABLE  
14  HOURS


HARD DRY    
18  HOURS


(THE DRYING TIME MAY VARY DEPENDING ON THE CLIMATIC CONDITION AND TYPE OF THINNER USED )

SOLID CONTENT
:
51﹪±2

VOC
:  <550g/l

SPREADING RATE
:  10－12 SQ METRES/LITRE

(TOTAL AREA MAY VARY DEPENDING ON THE NATURE OF WOOD AND THE SURFACE CONDITION )

THINNER  
:
PANDA BRAND 511 ECO THINNER


ACCORDING TO THE APPLICATION METHHOD AND CLIMATIC CONDITION, THE AMOUNT OF THINNER CAN BE VARIED TO MEET THE NEED OF APPLICATION.  SUGGEST NOT TO ADD EXCEED 15% OF THINNER.

APPLICATION 
:
BRUSH ROLLER OR SPRAY
SURFACE PRE-
:
NEW AND PREVIOUSLY PAINTED SURFACES SHOULD BE DRY AND FREE FROM 

PARATION
:
ANY LOOSE AND FLAKING MATERIAL, DIRT, GREASE, WAX AND POLISH.

PACK SIZE  
:
4 LT
PRECAUTION
:
INFLAMMABLE LIQUID
STORE & USE AWAY FROM HEAT AND FLAME 

ALLOW GOOD VENTILATION DURING APPLICATION
NOTE : All information is given in good faith and based upon results obtained from experiences and testing. However, all recommendations and suggestions are made without guarantee since conditions of use are beyond our control. We reserve the right at any time and without notice to update or improve our products and processes and our information concerning same. 
[image: image1.jpg]