[image: image1.jpg]l‘l" KRR R

WINSOME PAINTS CO., LTD.

ERNATBREAGIETBAI P 012042
Room 1204, Yuen Long Trading Centre, 33 Wang Yip Street West, Yuen Long, N.T. Hong Kong.
TEL: 24766844 FAX: 24730017





PRODUCT INFORMATION
PRODUCT CODE
:
E6900

PRODUCT NAME
:
PANDA BRAND ECO WHITE FLAT PAINT

DESCRIPTION
:
BASED　ON HIGH GRADE SYNTHETIC RESINS.  VISCOUS, HIGH OPACITY FLAT PAINT WITH GOOD BRUSHABILITY AND HOLDOUT. IT IS PARTICULARY SUITABLE FOR METAL PRIMER.

VEHICLE
:
SYNTHETIC RESINS
COLOUR
:
WHITE.

GLOSS
:
MATT

DRYING TIME
:
TOUCH DRY
3  
HOURS

RECOATABLE  
16 
HOURS

HARD DRY    
18~24
HOURS


(THE DRYING TIME MAY VARY DEPENDING ON THE CLIMATIC CONDITION AND TYPE OF THINNER USED )

SOLID CONTENT
:
68%±2

V O C
 
: <400g/L
SPREADING RATE
:
10~15 SQ METRES / LITRE

(TOTAL AREA MAY VARY DEPENDING ON THE SURFACE CONDITION )

THINNER 
: 
PANDA BRAND 511 ECO THINNER



ACCORDING TO THE APPLICATION METHOD AND CLIMATIC CONDITION, THE AMOUNT OF THINNER CAN BE VARIED TO MEET THE NEED OF APPLICATION. 

APPLICATION 
:
BRUSH, ROLLER OR SPRAY.
SURFACE PRE-
:
NEW AND PREVIOUSLY PAINTED SURFACES SHOULD BE DRY AND FREE FROM ANY PARATION LOOSE AND FLAKING MATERIAL, DIRT, GREASE, WAX AND POLISH.

PACK SIZE  
:
20 LT, 4 LT AND 1 LT
PRECAUTION
:
INFLAMMABLE LIQUID
STORE & USE AWAY FROM HEAT AND FLAME

ALLOW GOOD VENTILATION DURING APPLICATION
NOTE : All information is given in good faith and based upon results obtained from experiences and testing. However, all recommendations and suggestions are made without guarantee since conditions of use are beyond our control. We reserve the right at any time and without notice to update or improve our products and processes and our information concerning same.  

[image: image1.jpg]